Specifications for Rhino Perforated & Cushioned Tiles

Note:  Due to variations in recycled materials from shipment to shipment, the following specifications are a median description only.  Actual specifications with regard to density, brittleness, elongation and tensile strength may very as much as 15% above or below the median figures represented below.

Material:
100% Recycled cable grade PVC with UV stabilizers

Size:
12" x 12"

Thickness:
Approximately 3/4"

Weight:
Perforated (Showertile) 1.35 lbs;  Cushioned (Aerobitile) 1.5 lbs each

Colors:
Navy Blue, Royal Blue, Light Blue, Forest Green, Yellow, Dark Gray, Light Gray, Red, Black

Density (ASTM D792-88):
1.3gram/cc

Brittleness/Temp (ASTM D745-73):
-24 degrees C

Elongation (ASTM D638-77):
350%

Tensile Strength (ASTM D2863-77)
2000 psi

Flame Resistant (ASTM 648 - class 2, MFA 253, NBSIR 75-950): Yes

Waterproof:

Yes

Also resistant to: Oil, gasoline, most solvents, caustics, mold, mildew, water, ozone abrasion aging.            


         Retards development of bacteria. 

*Color and tensile strength not affected by heat, cold, humidity or sunlight (except red).

