**TEMP FLOOR**

**MODULE SIZE:**  **WIDTH** 6” 1 TILE = 1 SQUARE FOOT

**LENGTH** 24”

**THICKNESS** ¾”

**MODULE WEIGHT:** 1.1 LBS PER TILE/PER SQUARE FOOT

**MATERIAL:** HIGH-IMPACT POLYPROPYLENE CO-POLYMER

UV INHIBITORS ADDED.

**FIRE RATING:** ASTM E-648 DATA SHEET ATTACHED.

EXTENT OF FLAME TRAVEL (MM) 1070

CRITICAL RADIANT FLUX (W/cm sq.) IS 0.08

**SUPPORT STRUCTURE:** FLOORING MODULE INCORPORATES

MULTI-DIRECTIONAL STRUCTURAL SUPPORT

RIBBING, ALLOWING FOR DISTRIBUTION OF WEIGHT LOADS.

**WEIGHT LOADING:** 27,000 lbs/sqft

**GROUND SURFACES:** TEMP FLOOR’S UNIQUE HINGED DESIGN ALLOWS FOR USE ON UNEVEN

SURFACES-ON GRASS,SAND GRAVEL,CONCRETE,ASPHALT ICE,SNOW

ETC, WITH LITTLE SUB-SURFACE PREPARATION

**SHIPPING:**  40” x 48” PALLET

TEMP FLOOR IS DELIVERED PRE-ASSEMBLED IN 3” x 4”

PANELS [12 TILES TO A PANEL]

EACH PALLET CAN BE LOADED WITH UP TO 100 PANELS

[1200 TILES] OR 1200 SQ.FT. [3” x 4” x 8”] PALLET DIMENSIONS

20’ OCEAN CONTAINER 12,000 sq.ft.

40’ OCEAN CONTAINER 20,000 sq.ft.

48’ TRUCK 24,000 sq.ft.

53’ TRUCK 28,800 sq.ft

**FUNCTIONAL FEATURES:**

1. INDIVIDUAL MODULAR PANELS INTERCONNECT EASILY IN 12 sq.ft.

SECTIONS

1. TEMP FLOOR’S HINGE DESIGN ALLOWS FOR THE MODULES TO BE

ROLLED-UP FOR DISASSEMBLY IF SO DESIRED. 6’ x 20’ROLLS CAN BE

EFFICIENTLY HANDLED.

1. EACH TILE FEATURES AN ATTRACTIVE TEXTURED NON-SLIP SURFACE

WITH A MULTITUDE OF AERIATION HOLES FOR TEMPORARY USE ON

GRASS SURFACES.

1. EACH TILE INCORPORATES A HALF-MOON NETWORK OF CHANNELS TO

FACILITATE WATER FLOW IN RAIN SHOWER CONDITIONS AND/OR TO

FACILITATE POWER & COMMUNICATION WIRING.

**WARRANTY** 3 YEAR WARRANTY AGAINST MANUFACTURER’S DEFECTS UNDER

NORMAL USE CONDITIONS.